Chi3 of Metal for different pulse duration

---
Motivation: chi3 should change with pulse durations
[1] Robert W. Boyd, Zhimin Shi, and Israel De Leon. The third-order non-linear optical susceptibility of gold. Optics Communications, 326:74–79, 2014.

---
Former gold simulation
[1] Robert W. Boyd, Zhimin Shi, and Israel De Leon. The third-order non-linear optical susceptibility of gold. Optics Communications, 326:74–79, 2014.

---
Check back for the original formula!
[2] G. F. Bertsch, J.-I. Iwata, Angel Rubio, and K. Yabana. Real-space, real-time method for the dielectric function. Phys. Rev. B, 62:7998–8002, Sep, 2000

---
exp(- eta t) envelope
1. exp(eta t) works for the kick delta function, but not suitable for our continuous laser pulse!
2 . It can converge the edge of Fourier transformation range, avoid strange peaks after FT!
3. When we increase the propagation time, we can get nothing more new information, they all lost!

---
A new envelope for continuous wave
10 fs sin^2 head + arbitrary flat pulse duration + 10 fs sin^2 tail
\eta = 0
Derivative smooth
No singularity

---
Further formulas
[3] Raúl del Coso and Javier Solis. Relation between nonlinear refractive index and third-order susceptibility in absorbing media. J. Opt. Soc. Am. B, 21(3):640–644, Mar 2004

---
Iridium: pulse duration = 1000, 2000, 3000 [hbar/Ha], A = 2 [Ha]
Gauge field A

---
Iridium: pulse duration = 1000, 2000, 3000 [hbar/Ha], A = 2 [Ha]
dA/dt Derivative smooth, No singularity

---
Iridium: pulse duration = 1000, 2000, 3000 [hbar/Ha], A = [ 1.2, 1.4, 1.6, 2, 2.1, 2.3, 2.6, 3] [Ha]
FT{Eext} FT{Eind} Intensity without modification

---
Iridium: pulse duration = 1000, 2000, 3000 [hbar/Ha], A = [ 1.2, 1.4, 1.6, 2, 2.1, 2.3, 2.6, 3] [Ha]
Dielectric function epsilon

---
Iridium: pulse duration = 1000, 2000, 3000 [hbar/Ha], A = [ 1.2, 1.4, 1.6, 2, 2.1, 2.3, 2.6, 3] [Ha]
Refractive index n, k
FT-- same for exp(iwt) or exp(-iwt)

---
Iridium: A = [ 1.2, 1.4, 1.6, 2, 2.1, 2.3, 2.6, 3] [Ha] Linear fitting

---
Iridium: A = [ 1.2, 1.4, 1.6, 2, 2.1, 2.3, 2.6, 3] [Ha]
Polynomial fitting!

---
Iridium: A = [ 1.2, 1.4, 1.6, 2, 2.1] [Ha] Linear fitting

---
Iridium: A = [ 2.1, 2.3, 2.6, 3] [Ha] Linear fitting

---
Gold polynomial fitting A =[10,20,30,40]

---
Gold polynomial fitting with A =[20,30,40]
 A=10 divergent, delete it!

---
Gold Add the envelope

---
Gold on Calculating!
Propagation time 50,000 au = 1200 fs ~ 10^{-12} s
5 Amplitudes! A = 0.1, 0.7, 1.2, 1.6, 2
5 Intensity [GW/cm^2] 0.08, 4.02, 11.82, 21.01, 32.82